SECTION 05 15 00

WIRE ROPE ASSEMBLIES-STAINLESS STEEL

Show hidden Specifier Notes for best results

I-SYS® INOX Brand stainless steel wire rope assemblies by:

Carl Stahl-DecorCable Innovations LLC;

660 W. Randolph St.

Chicago, IL USA 60661

Phone:  800-444-6271

Fax: 312-474-1789

E-mail: sales@decorcable.com

Web: www.decorcable.com

This Product Specification is written in accordance with the Construction Specifications Institute (CSI) Format , including MasterFormat, SectionFormat and PageFormat. Optional text is indicated by brackets [ ]; delete optional text in final copy of specification. Specifier Notes are shown in red typically precede specification text; delete Specifier Notes in final copy of specification.

This Section specifies stainless steel wire rope assemblies marketed under the I-SYS® tradename. Revise section number and title below to suit project requirements, local building codes, specification practices and section content. Refer to CSI MasterFormat for other section numbers and titles.

© 2006 Carl Stahl-DécorCable Innovations LLC

PART 1 GENERAL

# SUMMARY

## Section Includes:

### I-SYS Stainless Steel Wire Rope Assemblies

### I-SYS Stainless Steel Fittings, End Terminals, Hardware, and Accessories

## Related Sections:

Specifier Note: Edit following list according to project requirements.

### Section 4 - Masonry Anchoring and Reinforcing

### Section 5 - Metal Stairs

### Section 5 - Metal Railings

### Section 5 – Stainless Steel Wire Rope Assemblies

### Section 5 – Decorative Metal Railings

### Section 5 – Rooftop Fall Protection

### Section 32 – Site Improvements

# SYSTEM DESCRIPTION

## Performance Requirements: Provide Stainless Steel Cable Railing System and mounting hardware which have been manufactured and installed to meet or exceed manufacturer’s and project performance criteria.

# SUBMITTALS

Specifier Note: This Section includes submittal of relevant data to be furnished by Contractor before, during or after construction. Coordinate this article with Architect’s and Contractor’s duties and responsibilities in Conditions of the Contract and Division 1 Submittal Procedures Section.

## Submit listed submittals in accordance with Conditions of the Contract and Division 1 Submittal Procedures Section.

## Product Data: Submit Manufacturer’s product data sheet for specified products.

## Shop Drawings: Show layout, sizes, dimensions, details, and installation of railing frame components. Include Details of rope attachment, tensioning methods, hardware, and tensioning and mounting methodology.

## Samples: Submit samples of rope and/or hardware, as required by specifier.

## Quality Assurance/Control Submittals:

### Test reports: Submit any test report demonstrating compliance with intended use and code requirements.

### Certificates: Submit manufacturer’s certificate that product meets or exceeds specified requirements

## Closeout Submittals: Submit the Following:

### Warranty: Submit manufacturer’s standard warranty documents

### Maintenance Data: Include manufacturer’s standard cleaning and maintenance instructions to avoid detrimental actions to finishes and performance.

# QUALITY ASSURANCE

Specifier Note: This Section should include prerequisites, standards, limitations and criteria that establish an overall level of quality for products and workmanship for this section. Coordinate with Division 1 Quality Assurance Section.

## Qualifications:

### Installer Qualifications: Installer should be experienced in performing work of this section and should have specialized in installation of work similar to that required for this project.

## Regulatory Requirements and Approvals:

### [Code Agency Name]

#### [Report or Approval Description]

## Mock-Ups: Install at project site or appropriate location a job mock-up using acceptable products and manufacturer approved installation methods. Obtain Owner’s and Architect’s approval of product, application, and workmanship standards. Comply with Division 1 Quality Control (Mock-Up Requirements) Section.

Specifier Note: Edit paragraph below when specifying mock-up requirements.

### Mock-Up Size: [Specify mock-up size and fixation requirements].

### Maintenance and Disposal: Maintain mock-up during construction for workmanship comparison.

Delete one of the following two choices for final disposition of mock-up

#### Removal: Remove and legally dispose of mock-up when no longer required.

#### Incorporation: Mock-up may be incorporated into final construction upon Owner’s approval.

## Pre-Installation Meetings: Conduct with [Contractor, Architect, Fabricator, Installer and any other subcontractors] whose work involves cable railing system to verify project requirements, framing and support conditions, mounting surfaces, manufacturer's installation instructions, and warranty requirements.  Comply with Division 1 requirements.

# DELIVERY, STORAGE, AND HANDLING

Specifier Note: This Section should include special and unique product requirements. Coordinate article below with Division 1 Product Requirements Section.

## General: Comply with Division 1 Product Requirements Sections Ordering: Comply with manufacturer’s ordering instructions and lead time requirements to avoid construction delays.

## Delivery: Deliver in manufacturer's original, unopened, undamaged containers, identification labels intact.

## Storage and Protection: Store materials protected from exposure to harmful weather conditions and at temperature and humidity conditions recommended by manufacturer. Store cartons and panels in a secure location in a dry place at the project site.

# WARRANTY

Specifier Note: Coordinate article below with Conditions of the Contract and with Division 1 Closeout Submittals (Warranty) Section.

## Manufacturer’s Warranty: Submit, for Owner’s acceptance, manufacturer’s standard warranty document executed by authorized company official.

PART 2 PRODUCTS

Specifier Note: Retain article below for proprietary method specification. Add product attributes, performance characteristics, material standards and descriptions as applicable. Use of such phrases as “or equal” or “or approved equal” or similar phrases may cause ambiguity in specifications. Such phrases require verification (procedural, legal and regulatory) and assignment of responsibility for determining “or equal” products.

# I-SYS® INOX STAINLESS STEEL WIRE ROPE ASSEMBLIES

## Manufactured and sold by: Carl Stahl DécorCable Innovations, Inc., 2401 International Pkwy., Ste. B, Woodridge, IL USA 60517. Tel: 312-474-1100, Fax: 312-474-1789, E: sales@decorcable.com, Web: www.decorcable.com.

## Proprietary Products/Systems: I-SYS® INOX Brand Stainless Steel Wire Rope Assemblies.

### Material:

#### Cable: Type 316 stainless steel 7x7 or 7x19 wire rope, or 1x19 strand.

#### Fittings, Hardware, and Accessories: AISI 304, 316 or 316L stainless steel

Specifier Note: 7x7 and 7x19 wire rope is suitable for most general non-structural applications due to ease of use and excellent flexibility to bends and curves. 1x19 has higher tensile capacity per diameter and is more resistant to bending and deformation under load. Large diameter stranded constructions can be certified for structural use and require special end fittings and terminals. Select required rope construction in Section 2 below and the appropriate fittings, hardware and accessories in Sections 3, 4, 5, and 6 to specify your assemblies. Follow assembly length guidance in Section 7. Delete paragraphs not required. Contact Carl Stahl-DecorCable for assistance in determining the correct cable and end fittings for your application.

### Rope Stock Number, Composition, Diameter, Min. Breaking Load (MBL) and MQ (mm²):

#### General Use 7x7 rope construction:

#### #820-0100- ø 1mm (3/64”),	56 lbs. MBL, 	.43mm² MQ

#### #820-0200- ø 2mm (5/64”),	501 lbs. MBL, 	1.71mm² MQ

#### #820-0300- ø 3mm  (1/8”), 	1120 lbs. MBL,	3.85mm² MQ

#### #820-0400- ø 4mm  (5/32”),	2000 lbs. MBL, 6.85mm² MQ

#### #820-0500- ø 5mm  (3/16”),	3135 lbs. MBL, 10.70mm² MQ

#### #820-0600- ø 6mm  (1/4”), 	4500 lbs. MBL, 15.42mm² MQ

#### #820-0800- ø 8mm  (5/16”), 8020 lbs. MBL, 	27.40mm² MQ

#### General Use, High Flexibility 7x19 rope construction:

#### #830-0200- ø 2mm  (5/64”), 636 lbs. MBL, 	1.66mm² MQ

#### #830-0300- ø 3mm  (1/8”), 1050 lbs. MBL, 	3.73mm² MQ

#### #830-0400- ø 4mm  (5/32”), 1868 lbs. MBL, 	6.63mm² MQ

#### #830-0500- ø 5mm  (3/16”), 2912 lbs. MBL, 10.36mm² MQ

#### #830-0600- ø 6mm  (1/4”), 4210 lbs. MBL, 14.92mm² MQ

#### #830-0800- ø 8mm  (5/16”), 7480 lbs. MBL, 26.53mm² MQ

#### #830-1000- ø 10mm (13/32”), 11670 lbs. MBL, 41.45mm² MQ

#### #830-1200- ø 12mm (15/32”), 16822 lbs. MBL, 59.69mm² MQ

#### #830-1400- ø 14mm (9/16”), 22848 lbs. MBL, 81.25mm² MQ

#### #830-1600- ø 16mm (5/8”), 29790 lbs. MBL, 106.12mm² MQ

#### General Use, Higher Stiffness and Strength 1x19 stranded construction:

#### #810-0200- ø 2mm  (5/64”), 736 lbs. MBL, 2.39mm² MQ

#### #810-0300- ø 3mm  (1/8”), 1662 lbs. MBL, 5.37mm² MQ

#### #810-0400- ø 4mm  (5/32”), 2956 lbs. MBL, 	9.55mm² MQ

#### #810-0500- ø 5mm  (3/16”), 4614 lbs. MBL, 14.92mm² MQ

#### #810-0600- ø 6mm  (1/4”), 6652 lbs. MBL, 21.49mm² MQ

#### #810-0800- ø 8mm  (5/16”), 11065 lbs. MBL, 38.20mm² MQ

#### #810-1000- ø 10mm (13/32”), 17292 lbs. MBL, 59.69mm² MQ

#### #810-1200- ø 12mm (15/32”), 23296 lbs. MBL, 85.95mm² MQ

#### #810-1400- ø 14mm (9/16”), 29344 lbs. MBL, 116.99mm² MQ

#### #810-1600- ø 16mm (5/8”), 39424 lbs. MBL, 152.81mm² MQ

#### #810-1900- ø 19mm (3/4”), 52192 lbs. MBL, 215.48mm² MQ

#### #810-2200- ø 22mm (7/8”), 66976 lbs. MBL, 288.90mm² MQ

#### #810-2600- ø 26mm (/32”), 93184 lbs. MBL, 403.51mm² MQ

#### Structural Use, Very High Stiffness/Strength 1x37 or 1x61 stranded construction. May require special hardware and end fittings. Consult catalog or Carl Stahl-DecorCable.

#### #610-1600- ø 16mm (5/8”), 1 x 37, 41350 lbs. MBL, 150.80mm² MQ

#### #610-1800- ø 18mm (23/32”), 1 x 37, 50960 lbs. MBL, 190.80mm² MQ

#### #610-2200- ø 22mm (7/8”), 1 x 61, 72128 lbs. MBL, 285.10mm² MQ

#### #610-2600- ø 26mm (/32”), 1 x 61 99680 lbs. MBL, 398.20mm² MQ

Specifier Note: Swaged stainless steel ends fittings are permissible for both SS Wire Rope and Strand Constructions. Field Installed stainless steel ends are permissible for SS Rope, only. Minimum Breaking Strength: 90 percent of cable MBR. Swaged ends provide ultimate holding strength and smallest fitting size for all rope diameters. Field installed fittings are normally slightly larger in diameter with holding strength approaching swaged fittings. See our catalog for technical details.

### Swaged and Field Installed End Fittings and Terminals:

#### Easy Grip Internal Thread – Stock #760, LH #761

#### Internal Thread Swageless Connection – Stock #831, LH #832

#### Internal Thread Swivel Swaged – Stock #857

#### Internal Thread Swaged – Stock #860, LH #861

#### External Thread Swaged – Stock #850, LH #855

#### External Thread Swivel Swaged – Stock #856

#### External Thread F30 Hammered – Stock #948, LH # 949

#### External Thread F50 Hammered – Stock #950, LH #951

#### External Thread Roll Swaged – Stock #650, LH #655

#### Fork Roll Swaged – Stock #681

#### Turnbuckle With Fork Fitting – Stock #670

#### Fork With Internal Thread Swaged – Stock #306, LH #307

#### CS Fork With External Thread Hammered – Stock #346, LH #345

#### Turnbuckle With Fork Fitting – Stock #670

#### Fork Roll Swaged – Stock #681

#### BW Fork Swageless Connection – Stock #754

#### Fork With Internal Thread Swaged – Stock #812, LH #811

#### Turnbuckle With Fork Hammered – Stock #870

#### Turnbuckle With Fork Swaged – Stock #870

#### Fork Swaged – Stock #881

#### CS Fork Swaged – Stock #947

#### Eye With Internal Thread Swaged – Stock #814, LH #813

#### CS Eye With Internal Thread Swaged -  Stock #816, LH #815

#### Eye Swaged – Stock #880

#### Turnbuckle With Eye Hammered – Stock #889

#### Turnbuckle With Eye Swaged – Stock #889

#### CS Eye Swaged -Stock #980

#### Radius Head With External Thread Hammered – Stock #170

#### Countersunk Head With External Thread Hammered – Stock #180

#### Ball Head With External Thread Hammered – Stock #190

#### End Stop Swaged – Stock #865

#### End Stop Countersunk 90° Round Swaged – Stock #866

#### End Stop With Countersunk 90° Swaged – Stock #866

#### End Stop With radius Head Swaged – Stock #869

#### End Stop With Radius Head Round Swaged – Stock #869

#### Loop Swaged Without Thimble – Stock  #803

#### Loop Swaged With Thimble – Stock #804

Specifier Note: Assembly lengths over to 20-25 feet normally require additional tensioning capacity. Add In-Line Tension Devices for every 20-25 feet of rope length. See our catalog or contact Carl Stahl-DecorCable for more details.

### In-Line Tension Devices:

#### Turnbuckle With Thread Hammered – Stock #110

#### Turnbuckle With Thread Swaged – Stock #110

#### Turnbuckle Cylindrical With Thread F30 Hammered – Stock #130

#### Turnbuckle F50 Hammered – Stock #824

#### Turnbuckle Swageless Short – Stock #825

#### Turnbuckle Swageless – Stock #825

#### Turnbuckle Threads F30 Hammered – Stock #828

#### Turnbuckle Threads Swaged – Stock #829

#### Turnbuckle Roll Swaged – Stock #625

#### Turnbuckle – Stock #675

#### Turnbuckle With Two Forks – Stock #8712

Specifier Note: Threaded fittings such as forks, eyes and loops facilitate secure attachment and tensioning of rope assemblies to support structure and require an internal or external thread end be already attached to the rope. See our catalog or contact Carl Stahl-DecorCable for more details

### Fittings with External and Internal Threads

#### External Thread Roll Swaged- Stock #650, LH Stock #655

#### External Thread Swageless Connection – Stock #826, LH #827

#### Fork With External Thread – Stock #671, LH #672

#### Fork With Internal Thread – Stock #817, LH #818

#### Turnbuckle With Fork Swageless – Stock #870

#### Fork With External Thread – Stock #871, LH #872

#### CS Fork With Internal Thread – Stock #917, LH #918

#### CS Fork With External Thread – Stock #945, LH #946

#### Eye With Internal Thread – Stock #806, LH #807

#### Eye With External Thread Bended – Stock #885, LH #886

#### Eye With External Thread – Stock #885, LH #886

#### Eye Counterpiece – Stock #887

#### Eye Bolt – Stock #888

#### CS Eye With Internal Thread – Stock #906, LH #907

#### CS Eye With External Thread – Stock #985, LH #986

#### Countersunk Stop With Internal Thread – Stock #866

#### Ball Head With Internal Thread – Stock #868

#### Radius Head End Stop With Internal Thread – Stock #869

Specifier Note: Specify necessary clamps, hardware, and accessories the ensure proper and secure installation and stabilization of rope assemblies. See our catalog or contact Carl Stahl-DecorCable for more details

### Clamps, Hardware, Accessories:

#### Pivot Base For Ball Head Flat Profile – Stock #868

#### Pivot Base For Ball Head Round Profile – Stock #868

#### Wire Rope Grip, Heavy TYP – Stock #800

#### Adjustable Screw On Cross Clamp – Stock #858

#### Cross Clamp 90° - Stock #858

#### Cross Clamp Adjustable – Stock #858

#### Cross Clamp With Internal Thread Adjustable – Stock #858

#### CS Cross Clamp Adjustable – Stock #858

#### Cross Clamp With Connection – Stock #858

#### Screw On Cross Clamp – Stock #858

#### Cover Disk For Rope Clamp Cone – Stock #859

#### Rope Clamp Cone – Stock #859

#### Angle Stand Off Washer – Stock #859

#### Light Clamp Ring With Adapter – Stock #869

#### Light Clamp Ring – Stock #863

#### Two Part Clamp Ring – 873

#### Light Clamp Ring With Thimble – Stock #874

#### Loop Clamp Ring With Thimble – Stock #874

#### Rod/Rope Holder – Stock #921

#### Rope Guiding Fork Head – Stock #921

#### Rope Pulley Block – Stock #921

#### Thimble – Stock #5970

#### Rod With Both Sides Threaded, RH or LH – Stock #IS

#### Rampa Screw For Wood – Stock #803

#### Wall Anchor Z-IG-A4 – Stock #803

#### Wall Anchor – Stock #803

#### Fork Bracket – Stock #834

#### Bow Shackle – Stock #835

#### Shackle D-Form – Stock #835

#### Cover Disk With Internal Thread or Through Hole – Stock #836

#### Eye Bold – Stock #837

#### Eye Nut – Stock #838

#### Hexagon Head Screw – Stock #843

#### Socket Head Screw – Stock #844

#### Angle Stand Off Washer For External Thread Flat Profile – Stock #862

#### Angle Stand Off Washer For External Thread Round Profile – Stock #862

#### Angle Washer For Countersunk End Stop 90° Flat Profile – Stock #862

#### Angle Washer For Countersunk End Stop 90° Round Profile – Stock #862

#### Loose Sleeve – Stock #864

#### Turnbuckle Cylindrical, Left/Right – Stock #875

#### Turnbuckle Left/Right – Stock #875

#### Thread Sleeve _ Stock #876

#### Dual Thread Screw – Stock #878, LH #877

#### Threaded Rod – Stock #882, LH #883

#### Headless Screw RH/LH – Stock #884

#### Pan Head Screw – Stock #890

#### Hexagon Nut – Stock #892, LH 893

#### Lock Nut With Nylon Insert – Stock #892

#### Dome Nut – Stock #894

#### Washer – Stock #896

#### Ball End With Internal Thread – Stock #898

#### Ball For Internal Thread Radius Head – Stock #899

#### Wire Rope End Cap – Stock #904

#### Washer For Wood – Stock #896

#### Wall Anchor For External Thread – Stock #30803

#### Wall Anchor With Internal Thread – Stock #30803

Specifier Note: Contact Carl Stahl-DécorCable salesperson or website for measurement templates and guidelines at 312-474-1100 or go to www.decorcable.com.

### Length:

#### Provide optimum adjustment in both directions by calculating final tendon lengths with allowance for tensioning fittings with 2/3 open and with 1/3 of thread length engaged.

#### Measure tendon length from center of pin to center of pin, or center of eye to center of eye.

# PRODUCT SUBSTITUTIONS

## Substitutions: No substitutions permitted.

# FITTINGS AND ACCESSORIES

## Accessories: Provide grommet, bushings, nuts, washers, turnbuckles, fittings and other components as required for system installation

# FABRICATION

## Stainless Steel Cables and Fittings shall be dimensioned and fabricated to specified size and labeled according to shop drawings and installer’s specifications.

## Preassemble items in shop to greatest extent practicable to minimize assembly at project site. Disassemble units only to extent necessary for shipping and handling limitations. Mark units for reassembly.

PART 3 EXECUTION

Specifier Note: Article below is an addition to the CSI SectionFormat. Revise article below to suit project requirements and specifier’s practice.

## MANUFACTURER’S INSTRUCTIONS

## Compliance: Comply with manufacturer’s product data, including product technical bulletins, product catalog installation instructions and product carton instructions for installation.

Specifier Note: Specify actions required to physically determine that conditions are acceptable to receive primary products of the section.

## EXAMINATION

## Site Verification of Conditions: Verify condition existing support system which has been previously installed under other sections, to ensure it is acceptable for product installation in accordance with manufacturer’s instructions. Do not begin installation until backup surfaces are in satisfactory condition.

## PREPARATION

## Supply items required to be cast into concrete or embedded in masonry with setting templates, to appropriate sections.

## Take field measurements after permanent end terminations are in place and prior to preparation of shop drawings and fabrication, to ensure fitting of work.

## INSTALLATION

## Install rope assemblies in accordance with manufacturer's instructions and the approved shop drawings.

## Provide anchorage devices and fittings to secure to in-place construction; including threaded fittings for concrete inserts, toggle bolts and through-bolts.

## Anchor rope assemblies to mounting surfaces as indicated on the drawings.

## Separate dissimilar materials with bushings, grommets or washers to prevent electrolytic corrosion.

## Use manufacturer’s supplied mounting hardware.

## Terminate and tension cable system in accordance with manufacturer’s instructions.

## Ensure ropes are clean, and without kinks or sags.

## After final adjustment provide tamper resistant locktight materials on all fittings.

## CLEANING

## Remove temporary coverings and protection of adjacent work areas.

## Clean installed products in accordance with manufacturer's instructions before owner's acceptance. Do not use chlorine-based or abrasive cleaners.

## Remove from project site and legally dispose of construction debris associated with this work.

## PROTECTION

## Protection: Protect installed product from damage during subsequent construction activities.

END OF SECTION